[image: ]
KPONE KATAMANSO MUNICIPAL ASSEMBLY
SPECIFICATION

PROJECT TITLE:	SUPPLY OF 4-NO. COMMUNAL SKIP CONTAINERS FOR THE KPONE KATAMANSO MUNICIPAL ASSEMBLY
PACKAGE NUMBER:	GAR/KKMA/DACF/GDS/RFQ/06/26



	NO. 
	DESCRIPTION
	REQUIRED 
	OFFER

	1
	TYPE OF STEEL MATERIAL 
	GALVANIZED 
	GALVANIZED 

	2
	SIDE PLATE
	4 MM
	4 MM

	3
	BASE PLATE
	5 MM
	5 MM

	4
	SIDE HOOK
	14 MM
	14 MM

	5
	2.5 X 1.5 U-CHANNEL
	11/2 X 21/2
	11/2 X 21/2

	6
	SHAFT
	18FT (2”) 
50 MM ROUND BAR X 5.5M
	18FT (2”) 
50 MM ROUND BAR X 5.5M

	7
	COATING 
	ANTIRUST (RED OXIDE)
	ANTIRUST (RED OXIDE)

	8
	COLOUR 
	GREEN (SPRAYING)
	GREEN (SPRAYING)
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